## Slide 1
Basic Inorganic Chemistry For B.Tech & B.Sc I yr
Main Group Chemistry
(2 lectures)
Silicones, silicates, aluminosilicates, zeolites and shape selective catalysis
Prepared by Prof. Anil J. Elias, IIT Delhi

## Slide 2
What makes silicon unique and its chemistry the choice of a wide range of environmentally friendly industrial applications ?
Applications in steel refining & Semiconductor industry
Inorganic polymer industry based on Silicones
Industry based on piezo electricity of quartz
Industry based on alumino silicates: from bricks, glass, cement to crockery
Zeolites as drying agents water softeners and unique catalysts
High natural abundance and easy availability of starting material (Sand) (silicon is the second most abundant element on the earth)
An easy purification process to pure silicon
A simple and cost efficient method for synthesis of organochlorosilanes and their polymerization to silicone polymers
Highly environmentally friendly end products with a diverse range of proven applications
Silicon, Silicone, Silicate, Aluminosilicate, Zeolites
and Shape Selective Catalysis
Taken from the earth : given back to the earth

## Slide 3
Isolation and Purification of the Element
The first step in making pure silicon is reduction of silica to an impure form of silicon known as ferrosilicon. Ferrosilicon is an iron-silicon alloy that contains varying ratios of elemental silicon and iron.
Ferrosilicon accounts for about 80% of the world's production of elemental silicon. Silicon has a high propensity to form bonds with oxygen and Ferrosilicon is primarily used by the steel industry to remove dissolved oxygen in steel melt.
Ultrapure silicon for solar cells and electronics
For solar cell fabrication one requires silicon of much higher purity (+99.9%). For electronics grade the purity required is even higher (99.9999999% ; known as 9 nines)

## Slide 4
How is ultrapure silicon made and processed ?

## Slide 5
Carbon versus
Silicon-
Bond Energies

## Slide 6
Silicone Polymers
Lowest glass transition temperature, Tg = -127 °C
Kipping coined the word silicone. In 1937, after 30 years of research, on the occasion of his retirement (Bakrerian lecture of the Royal Society) said “The prospect of any immediate and important advance in this section of organic chemistry does not seem to be very hopeful." In 1943 Dow Corning company took up industrial production of silicone polymers

## Slide 7
Early synthesis of organosilanes
First report 1863 Friedel and Craft using alkylzinc reagents
SiCl4 + m/2 ZnR2  RmSiCl4-m + m/2 ZnCl2
F. Stanley Kipping used first organozinc, followed by Wurtz coupling (Na) and later Grignard reagents to make organosilicon compounds.
In 57 research papers Kipping created the basis of organosilicon chemistry. He made mostly ethyl and phenyl organochlorosilanes as methyl chloride is a gas difficult to handle. First examples of silicone polymers (having ethyl and or phenyl groups) was reported by Kipping in 1904 and he described the products of his reaction as “sticky messes of no particular use!”

## Slide 8
The Direct synthesis: Rochow-Mueller Process (1940)
The economically viable alternative for Grignard method:
Modern synthesis of organochlorosilanes

## Slide 9
Polydimethylsilicone (PDMS)
Industrial synthetic routes

## Slide 10
Types of silicone polymers
Silicone fluids: Linear chain silicones with varying substituents on silicon
Silicone rubbers or elastomers: Crosslinked silicone fluids with or without a filler
Silicone resins: Highly branched

## Slide 11
Silicone fluids
Property Application
High thermal stability Heat transfer media
Good low temp performance refrigerant in cryostats
Low surface tension release agents
antifoams
antiflatulents
Water repellency water proofing, polishes
waterproof textiles
Antifriction lubricant
Good dielectric properties power transmission fluids
High oxygen permeability masks, contact lens
Non toxicity medical
Tolerance to skin and physiological cosmetics, ointments

## Slide 12
Industrial success of Silicones
First human foot print on moon
Moon temperature
(-153 to +107 °C)
Hydrophobicity Oxygen permeability
Wide temp range Low glass transition temp
Antifrothing Non toxicity

## Slide 14
The representation of tetrahedral silicates
The chemistry of silicates and aluminosilicates

## Slide 15
Be3Al2(SiO3)6.
(Mg, Fe)2SiO4
Mg3Si4O10(OH)2.
asbestos
aluminosilicates

## Slide 16
Three different forms of tecto silicates (framework silicates) 4 O shared
Pure silicate: quartz, vitreous silica, silica gel, Fumed silica
Aluminosilicates; (having tetrahedral Al replacing tetrahedral Si)
Feldspars Ultramarines Zeolites
Sodalite cage
Na8S2(Al6Si6O24)
Igneous rocks
K(AlSi3O8)
Linde A ( Mol sieves 4A)
Na6(Al6Si6O24). 2H20
Blue due to S3 radical anion

## Slide 17
Are porus solids
Have replaceable Na+ cations
Have channels which lead to cavities
Have water molecules in these cavities and channels
The channel and cavity size vary from zeolite to zeolite
Zeolites or Molecular Sieves

## Slide 18
imbalance

## Slide 19
Zeolite Structure: Framework Alumino silicates
When a tetrahedral silicon (IV) is replaced in a silicate by an tetrahedral aluminum(III), the framework attains an extra negative charge. This will be compensated by a cation such as Na+. Such compounds are termed framework aluminosilicates

## Slide 21
Platonic Solids
423 BC 347 BC
Archimedian Solids

## Slide 22
Octahedron
Truncated Octahedron
3 Dimensional Perspective of Zeolites:
Truncating an Octahedron !

## Slide 23
The inside cavity is known as α cage having 6 octagons
8 hexagons and 12 squares
Also known as β cage
8 hexagons and 6 squares
Lowenstein’s Rule:
The AlO4- tetrahedra are always interspersed with SiO4 tetrahedra
Or
Al-O-Al units does not occur in zeolites

## Slide 24
Sodalite Linde A Faujasite
not considered a zeolite (Molecular Sieves 4A)
β cages – directly linked through square faces = Sodalite
β cages – linked through square faces but with a D4R spacer = Linde A
β cages – linked through hexagonal faces but with a D6R spacer = Faujasite
STRUCTURE OF ZEOLITES

## Slide 25
ZSM-5: Zeolite Socony Mobil–5
is a zeolite belonging to the pentasil family of zeolites. Its chemical formula is Na3Al3Si93O192·16H2O. Patented by Mobil Oil Company in 1975, it is widely used in the petroleum industry as a heterogeneous
catalyst for hydrocarbon isomerization reactions.
ZSM-5 has a high silicon to aluminum ratio.
Channel size 5.4 x 5.6 Å
Al: Si ratio 1:31
5.1 x5.5 Å
Most well known zeolite catalyst

## Slide 26
Zeolite A or Linde-A
Zeolite Y or Faujasite
Channel size 4.1 Å
Al: Si ratio 1:1
Channel size 7.4 Å
Al: Si ratio 2:5
Na12(AlO2)12(SiO2)12. 27 H2O
Na2(AlO2)2(SiO2)5. 10 H2O
Used as an ion exchanger for water softening (in detergents) due to high Na+ content. Dehydrated form used for absorption of moisture and small volatile molecules. Reusable and environmentally safe
Catalysis of larger molecules. Metal complexes can be even made inside the cavities

## Slide 27
Si x% - Al y%
Cations Na, Ca
Polar
3-D entangled channels
Faujasite
Ring 12
ZSM 5
Si 93 %
non-polar
Hydrophobic
1-D channels
Ring 10
Linde A
Si 50% - Al 50%
Cations Na, Ca
Polar
3-D straight channels
Ring 8

## Slide 28: ZSM-5: Shape Selectivity in Catalysis

## Slide 29
Transition State Shape Selectivity,
some transition-state intermediates are too large to be accommodated within the pores/cavities of the zeolites, even though
diffusion of neither the reactants nor the products are restricted.
transalkylation of dialkylbenzenes
meta-xylene, 1,3,5- and 1,2,4-trialkylbenzene.

## Slide 30
ZSM-5 catalyst

## Slide 31: SHAPE SELECTIVE CATALYSIS - REACTANT, PRODUCT, TRANSITION STATE SELECTIVITY